| Electrical characteristics 4/5SF |
| --- |
|  | Voltage range (V) 0.7 / 1.6 V |
|  | Capacity at C rate (Ah) 14 |
|  | Specific energy (Wh/kg at C) 47 |
|  | Energy density (Wh/dm3 at C) 180 |
|  | Power in discharge (W at 30% SOC, 3 sec) 250 |
|  | Power in charge (W for 0 to 80% SOC) 120 |
|  | Specific power in optimal conditions (W/kg at 80% SOC) 900 |
|  | Typical specific power (W/kg at 30% SOC, 3 sec) 700 |
|  | Typical power density (W/dm3 at 30% SOC, 3sec) 2500 |

| Mechanical characteristics |
| --- |
|  | Cell Dimensions (mm) : Diam. x H 41 x 93 |
|  | Cell Weight (kg) 0.360 |
|  | Cell typical volume (dm3) 0.095 |

| Operating conditions |
| --- |
|  | Operating temperature range (°C) as given by the thermal management system -10 /+ 45 |
|  | Transport or storage temperature range (°C) - 40 /+ 50 |