| Electrical characteristics 4/5SF. |
| --- |
|  | Voltage range (V); 0.7 / 1.6 V. |
|  | Capacity at C rate (Ah); 14. |
|  | Specific energy (Wh/kg at C); 47. |
|  | Energy density (Wh/dm3 at C); 180. |
|  | Power in discharge (W at 30% SOC, 3 sec); 250. |
|  | Power in charge (W for 0 to 80% SOC); 120. |
|  | Specific power in optimal conditions (W/kg at 80% SOC); 900. |
|  | Typical specific power (W/kg at 30% SOC, 3 sec); 700. |
|  | Typical power density (W/dm3 at 30% SOC, 3sec); 2500. |

| Mechanical characteristics |
| --- |
|  | Cell Dimensions (mm) : Diam. x H; 41 x 93. |
|  | Cell Weight (kg); 0.360. |
|  | Cell typical volume (dm3); 0.095. |

| Operating conditions |  |
| --- | --- |
|  | Operating temperature range (°C) as given by the thermal management system; -10 /+ 45. |
|  | Transport or storage temperature range (°C); - 40 /+ 50. |